Chemical resistance

PVC floorings  Lino Fatra, Thermofix , Fatra Imperio are resistant  to non-oxidizing organic and mineral acids like: 
Hydrochloric acid, hydrofluoric acid, Nitric acid, Phosphoric acid, Acetic acid, Formic acid, Citric acid
Lactic acid, Sodium hydroxide

According to EN 423/EN ISO 26987 were tested chemicals, which are used as cleaning agents or are included in depurants : 
Synthetic detergent, Soap, Ammonia solution, Ammonium hydroxide, Hydrogen peroxide, Sodium hypochlorite, Sodium thiosulfate, Oxalic acid, Denaturated ethanol, Lacquer petroleum, Turpentine.

Our floorings are equally resistant against a number of solvents, in particular:
Hydrocarbons ( inc. Petrol, Diesel oil, Transformer Oil), Alcohols, Ether, Esther (Acetate), Glycol 
( glycerol), Formaldehyde

Visible stains are made by Sulphuric acid, Potassium permanganate, Silver nitrate and other heavily oxidizing solutions.

Resistance of these materials, which are commonly used in the household, kitchen, laboratory or in the hospital or pharmaceutic industry, were specifically tested: 
Furniture polish, Black coffee, Red wine, Dark beer, Black currant, Plum jam, Blueberry fruit  squash, tomato ketchup, Beetroot, Dark tea, Human blood, Methylene blue, Potassium permanganate, Phenolic disinfectant, Detergent, Vinegar, Sodium hydroxide solution, Sodium chloride solution.

It is important to note, that PVC flooring are generally not recommended for use with Acetone, Ketones ( inc. MEK) , Ethers and Aromatic and chlorinated hydrocarbons.

Special attention must be paid to coloring chemicals. Color stains or oxidized surfaces caused by chemicals, spilled glue or another substances, can be completely restored by machine cleaning - regarding to producer recommendation.